## Slide 1
Six Month Industrial Training
Public Works Department
(Buildings and Roads)
(Nawanshahr)
Civil Engineering Department
Submitted by Supervisor
Ajay Suman S.D.E Tarsem Raj
Civil Engineering (2010-2014) Asst. Er. Rajinder Singh
CE-100193
1183654

## Slide 2: Surveying
For the detailed layout plan of D.C complex Nawashahr is surveyed with Total station.
Temporary Adjustments of Total Station includes:
• Setting up the instrument.
• Levelling up.
• Elimination of the parallax.

## Slide 3: Working Steps for Total Station
First of all the instrument is set on the tripod and all the initial adjustments are performed like centering, levelling, focusing as performed on the ordinary thedolite.
After these adjustments, the initial coordinates are filled in the instruments like East (X),North (Y), Z, height of target height of instrument.
The instrument is oriented along north direction and the horizontal angle is set as zero so to have the horizontal angle w.r.t North.

## Slide 4: Total station

## Slide 5: Continued…
Then the target is set at the desired position and the instrument is transit towards the target and the target is bisected.
Then the button OBS (observation) is pressed and then the E, N, Z, Horizontal angle, vertical angle are displayed on the screen of the instrument which can be recorded in the memory of the instrument and the stored data can be extracted by connecting it to the computer through the software of the instrument.
Then with the data the plotting of the layout plan can be done with the any CAD software.

## Slide 6: Continued… Rough sketch prepared while entering the points in TS

## Slide 7: Bitumen Extraction (Determining Bitumen Content)
This test is done to determine the bitumen content as per ASTM 2172. The apparatus needed to determine bitumen content are -
i) Centrifuge extractor
ii) Miscellaneous – bowl, filter paper, balance and commercial benzene.
A sample of 500g is taken.

## Slide 8: Procedure
Place sample (weight ‘A’) into centrifuge extractor
Cover it with Benzene and then put filter paper to tightly cover it.
Start the centrifuge extractor, revolving slowly and gradually increase the speed until the solvent ceases to flow from the outlet.
Stop. Add 200ml benzene and repeat the procedure. Repeat the procedure at least thrice, so that the extract is clear and not darker than the light straw colour and record the volume of total extract in the graduated vessel.
Remove the filter paper from the bowl and dry in the oven at 110 + 5oC. After 24hours, take the weight of the extracted sample (Weight ‘B’).

## Slide 9: Continued…
Results
Bitumen content = [(A-B)/A]×100 %
[(800-730)/800]×100 = 8.75%
(weight ‘A’)= sample
(weight ‘B’)= Extracted sample
Repeat the test thrice and average the results.

## Slide 10: Aggregate Impact Test
Significance
This test assesses the suitability of aggregate as regards the toughness for use in pavement construction.
Suitability to be checked by laboratory tests.

## Slide 11: Procedure
Surface dry aggregates passing 12.5 mm and retained on 10 mm selected. 3.25 kg aggregate required for one test sample
Cylindrical measure filled with aggregates in 3 layers, tamping each layer 25 times
After leveling the aggregates at the top surface the test sample is weighed.
The cylinder with the test sample and plunger in position is placed on compression machine.
Load is applied at a rate of 4 tonnes per minute upto 40 tonnes.
The crushed aggregate is taken out, sieved through 2.36 mm IS sieve and weighed to get material passing.

## Slide 12: Continued…
Aggregate impact value = W2 / W1 x100
w2 = Weight of fines passing 2.36 mm
w1 = Weight of sample
Specifications
Type of pavement material/ layer | Aggregate impact value, max, %
WBM Sub-base course | 50
Cement Concrete Base course | 45
Bituminous Macadam, Base Course | 35
WBM Surface course | 30
Bituminous Wearing Surfaces | 30

## Slide 13: Los Angeles Abrasion Test
Significance
It is resistance to wear or hardness of aggregates
Road aggregates at the top subjected to wearing action
Under traffic loads abrasion/attrition action within the layers as well
To determine suitability, tests have to be carried out

## Slide 14: Procedure
Aggregates dried in oven at 105 -110 ° C. to constant Weight conforming to any one of the gradings.
(E.g. 1250 gm of 40-25 mm, 1250 gm of 25-20 mm, 1250 gm of 20-12.5 mm, 1250 gm of 12.5-10 mm, with 12 steel balls)
Aggregate weighing 5 kg or 10 kg is placed in cylinder of the machine (W1 gms)
Machine is rotated at 30-33 rpm for 500 revolutions
Machine is stopped and complete material is taken out.
Sieved through 1.7 mm sieve. Weight passing is determined by washing the portion retained, oven drying and weighing (W2 gms).

## Slide 15: Continued…
Aggregate abrasion value is determined as:
LAAV = W2 / W1 x100
(W2 = Weight of fines passing 1.7 mm
W1 = Weight of the sample)
Specifications
Type of Pavement Layer | L. A abrasion value, max, %
WBM Sub-base course | 60
WBM Base course with bit. 50 Surfacing, BM Base course | 50
WBM Surface course, BM binder Course | 40
Bituminous Carpet, SD, Cement Concrete surface course | 35
Bituminous/Cement concrete Wearing Course | 30

## Slide 16: SLUMP TEST
It is used for measuring the workability of fresh concrete and to check the uniformity of concrete from batch to batch.
On site slump test

## Slide 17: Continued…
Concrete is drawn in the slump cone in 3 layers and each layer is tamped for 25 times. Then the slump cone is removed and the height of concrete is measured in mm. Slump height comes out different as the w/c ratio varies in the concrete.
Thus slump test is a measure of consistency of wetness of the concrete mix.
The vertical mould by which the concrete of the mould subsides is called slump. The distacnce should be measured immediately after removing the mould and recorded.
The values, thus determined should be within the prescribed limits for different concrete works

## Slide 18: Prescribed limits for different concrete works
Types of work | Consistency Required | Quantity of water per bag of cement in ltrs. | Permissible slump value in mm.
Vibrated concrete work for piles, precast and moulded works | soft | 22.5 | 10 to 25
Mass concrete work in foundations, road pavement etc. | Medium of slightly stiff | 29.25 | 25 to 50
Bridge deck | Medium | 24.75 | 25 to 75
Ordinary reinforced concrete for beams and slabs etc. | Medium | 24.75 | 30 to 125
R.C.C footings walls | Soft | 22.5 | 50 to 100
Columns | Medium | 24.75 | 75 to 125
Concrete work under water | Medium or slightly stiff | 29.25 | about 230

## Slide 19: Sieve Analysis
Significance of Test
Each type of aggregate test requires a specified aggregate size (E.g. 10-12.5 mm for crushing test)
Each bituminous mix type has a recommended aggregate gradation (% passing 26.5 mm in 55 90 for GSB1). So aggregate is passed through a set of sieves to get material of various sizes

## Slide 20: Procedure
Bring the sample to an air dry condition either by drying at room temperature or in oven at a temperature of 100ᴼC to 110ᴼC.Take the weight of the sample.
Clean all the sieves and sieve the sample successively on the appropriate sieves starting with the largest.
Shake each sieve separately over a clean tray.
On completion of sieving note down the weight of material retained on each sieve

## Slide 21: Continued…
5) Report the results as cumulative percentage by weight of sample passing each of the sieves.

## Slide 22: California bearing ratio (CBR)
California bearing ratio is defined as the ratio (expressed as percentage) between the load sustained by the soil sample at a specified penetration of a standard plunger (50 mm diameter) and the load sustained by the standard crushed stones at the same penetration.
CBR is basically a measure of strength.
Simple test that compares the bearing capacity of a material with that of a well-graded crushed stone.

## Slide 23: Continued…
High quality crushed stone material should have a CBR of about 100%.
CBR value is the measure of resistance of material to the penetration of standard plunger under controlled density and moisture condition.
The CBR test can be made in the laboratory on undisturbed or remoulded soil samples.
The CBR value of sub grade is normally evaluated on a soaked sample compacted at optimum moisture content to maximum dry density.

## Slide 24: Procedure
plunger of 50 mm diameter is penetrate to a soil sample at the rate of 1.25 mm/min.
Force (load) required to cause the penetration is plotted against measured penetration.
The loads at 2.5 mm and 5 mm penetration are recorded and load corresponding to 2.5 mm or 5 mm penetration is expressed as a percentage of standard load sustained by the crushed aggregates at the same penetration to obtain CBR value.

## Slide 25: Standard Load values on crushed Stones for different Penetration values
Penetration, mm | Standard Load, kg | Unit Standard Load, kg/cm2
2.5 | 1370 | 70
5 | 2055 | 105
7.5 | 2630 | 134
10 | 3180 | 162
12.5 | 3600 | 183

## Slide 26: Load vs. penetration curve

## Slide 27: THANK YOU